#### PURASORB

ACTIVE CARBON

| # Inglês |  |  |
| --- | --- | --- |
| ## TECHNICAL DATA SHEET |  |  |
| Material | ### Active Carbon (Granular) |  |
| Grade | KS510GR |  |
| Type | Coconut Shell Based Steam Activated Granular Active Carbon |  |
| Typical Properties |  |  |
|  | Particle Size (ASTM D2862-92) ( 1.8 – 3 mm) | 12 x 40, / 8 x 30 U.S.mesh 8 x 16, / 6 x 12 U.S.mesh |
|  | Apparent density (ASTM D2854-89) | 480 g/l |
|  | pH of aqueous extract (ASTM D3838-86) | 8 |
|  | Ash content (ASTM D2866-94) | 3.5 % |
|  | Hardness (ASTM D3802-79) | > 97 % |
|  | Moisture as packed (ASTM D2867-91) | 3 % |
|  | Surface Area (B.E.T. method) | 1050 m2/g |
|  | Iodine No. (JIS K1470-67) | 1000 mg/g |
|  | Methylene Blue (Spectrophotometric) | 20 g / 100g |
|  | CCl4 adsorption (ASTM D3467-94) | 50 % |
|  | Phenol value (CEFIC) | 1.8 g/l |
|  | Dechlorination half length (DIN19603) | 2.5 cm |
| Product Key Features |  |  |
|  | KS510GR has excellent adsorptive properties because of its high surface area and pore structure which is rich in micropores. The raw material and the activation method result in a carbon virtually free from dust with a very low ash content and high mechanical resistance. KS510GR absorbs a wide range of organic contaminants including micro-pollutants, THM’s, phenol compounds and free chlorine. It has applications in both drinking water treatment and industrial processes. |  |

#### PURASORB

##### CARVÃO ACTIVADO

| # Português |  |  |
| --- | --- | --- |
| FOLHA DE DADOS TÉCNICOS: |  |  |
| Material | Carvão Activado (Granular) |  |
|  | KS510GR |  |
| Tipo | Carvão activado em vapor, Granulado, com base em Casca de Coco |  |
| Propriedades Típicas |  |  |
|  | Tamanho da Partícula (ASTM D2862-92) ( 1.8 – 3 mm) | 12 x 40, / 8 x 30 U.S.mesh 8 x 16, / 6 x 12 U.S.mesh |
|  | Densidade aparente (ASTM D2854-89) | 480 g/l |
|  | pH da mistura aquosa (ASTM D3838-86) | 8 |
|  | Conteúdo em cinzas (ASTM D2866-94) | 3.5 % |
|  | Dureza (ASTM D3802-79) | > 97 % |
|  | Mistura quando embalado (ASTM D2867-91) | 3 % |
|  | Área Superficial (Método B.E.T.) | 1050 m2/g |
|  | Nº Iodo (JIS K1470-67) | 1000 mg/g |
|  | Azul de Metileno (Espectrofotómetro) | 20 g/100 g |
|  | Adsorção por CCl4 (ASTM D3467-94) | 50 % |
|  | Valor Fenol (CEFIC) | 1.8 g / l |
|  | Comprimento de meia desclorização (DIN19603) | 2.5 cm |
| Principais Utilidades do Produto |  |  |
|  | O produto KS510GR tem excelentes propriedades de adsorção devido á sua elevada área superficial e á sua estrutura porosa, rica em microporos. Da sua constituição e do seu método de activação resulta um carvão praticamente livre de pó, com um conteúdo muito baixo em cinzas e com uma resistência mecânica elevada. O KS510GR absorve uma vasta gama de contaminantes orgânicos, tais como os micro-poluentes, THM, compostos fenólicos e cloro livre. É aplicado no tratamento de água para beber e em processos industriais. |  |