#### PURASORB

#### ACTIVE CARBON

| # Inglês |  |  |
| --- | --- | --- |
| ## TECHNICAL DATA SHEET ###### AIR TREATMENT |  |  |
| Material | ### Active Carbon (Cylinders) |  |
| Grade | KS730GR |  |
| Type | Steam Activated Carbon produced from selected raw materials and extruded into cylinders |  |
| Typical Properties |  |  |
|  | Pellet diameter | 3 – 4 mm |
|  | Apparent density (ASTM D2854-89) | 520 g/l |
|  | Ash content (ASTM D2866-94) | 10 % |
|  | Hardness (ASTM D3802-79) | > 97 % |
|  | Moisture as packed (ASTM D2867-91) | 8 % |
|  | Surface Area (B.E.T. method) | 1050 m2 / g |
|  | Iodine No. (JIS K1470-67) | 1000 mg / g |
|  | CCl4 adsorption (ASTM D3467-94) | 45 % |
| Product Key Features |  |  |
|  | KS730GR adsorbs a wide range of volatile organic compounds including chlorinated solvents, hydrocarbons and high molecular weight mercaptans. KS730GR, as a result of its high retentivity and surface area is especially suited for air or gas purification with concentrations of organic solvents and odour removal. |  |
| Further Information |  |  |
|  | Specific enquiries relating to the application and use of active carbon may be directed to |  |

##### PURASORB

CARVÃO ACTIVADO

| # Português |  |  |
| --- | --- | --- |
| FOLHA DE DADOS TÉCNICOS: ###### TRATAMENTO DE AR |  |  |
| Material | ### Carvão Activado (Cilíndrico) |  |
|  | KS730GR |  |
| Tipo | Carvão activado em vapor, produzido a partir de matérias primas seleccionadas e extrudidas cilindricamente. |  |
| Propriedades Típicas |  |  |
|  | Diâmetro da Palet | 3 – 4 mm |
|  | Densidade aparente (ASTM D2854-89) | 520 g/l |
|  | Conteúdo em cinzas (ASTM D2866-94) | 10 % |
|  | Dureza (ASTM D3802-79) | > 97 % |
|  | Humidade quando embalado (ASTM D2867-91) | 8 % |
|  | Área Superficial (Método B.E.T.) | 1050 m2 / g |
|  | Nº Iodo (JIS K1470-67) | 1000 mg / g |
|  | Adsorção por CCl4 (ASTM D3467-94) | 45 % |
| Principais Utilidades do Produto |  |  |
|  | O produto KS730GR adsorve uma variada gama de compostos orgânicos voláteis, incluindo solventes clorídricos, hidrocarbonetos e mercaptans de elevado peso molecular. Como resultado da sua elevada retentividade e área superficial o KS730GR é especialmente indicado para purificação de ar ou gás, com concentração de solventes orgânicos e para remoção de odores. |  |
| Outras Informações |  |  |
|  | Perguntas específicas relacionadas com a aplicação e uso do carvão activado podem ser dirigidas a: |  |