#### PURASORB

#### ACTIVE CARBON

| # Inglês |  |  |
| --- | --- | --- |
| ## TECHNICAL DATA SHEET |  |  |
| Material | ### Active Carbon (Granular / MIXER) |  |
| Grade | KS 630 GR |  |
| Type | Mineral and vegetal Steam Activated Granular Active Carbon |  |
| TypRcal operties |  |  |
|  | Particle Size (ASTM D2862-92) ( 1.8 – 3 mm) | 12 x 40, / 8 x 30 U.S.mesh 8 x 16, / 6 x 12 U.S.mesh |
|  | Apparent density (ASTM D2854-89) | 497 g/l |
|  | pH of aqueous extract (ASTM D3838-86) | 7 |
|  | Ash content (ASTM D2866-94) | 0,5 % |
|  | Hardness (ASTM D3802-79) | > 97 % |
|  | Moisture as packed (ASTM D2867-91) | < 3 % |
|  | Surface Area (B.E.T. method) | 1050 m2/g |
|  | Iodine No. (JIS K1470-67) | 1000 mg/g |
|  | Methylene Blue (Spectrophotometric) | 20 g / 100g |
| Product Key Features |  |  |
|  | *** Range of granular activated carbons designed for adsorption of chloride and organic contaminants dissolved in water. *** Manufactured from select grades of mineral and vegetal activated carbons, with a thermal activation process at strictly controlled temperature to obtain a large residual area structure allowing the retention of a low and high molecular weight organic compounds.. *** High density activated carbon with a good resistance to attrition and mechanical pressure PURASORB KS 630GR Activated carbon require periodic backwashing to eliminate accumulated matters before returning to the filter. |  |
| Further |  |  |

#### PURASORB

##### CARVÃO ACTIVADO

| # Português |  |  |
| --- | --- | --- |
| FOLHA DE DADOS TÉCNICOS: |  |  |
| Material | Carvão Activado (Granular /MIXER) |  |
|  | KS5 630 GR |  |
| Tipo | Carvão Mineral e vegetal Granulado Ativado em Vapor |  |
| Propriedades Típicas |  |  |
|  | Tamanho da Partícula (ASTM D2862-92) ( 1.8 – 3 mm) | 12 x 40, / 8 x 30 U.S.mesh 8 x 16, / 6 x 12 U.S.mesh |
|  | Densidade aparente (ASTM D2854-89) | 497 g/l |
|  | pH da mistura aquosa (ASTM D3838-86) | 7 |
|  | Conteúdo em cinzas (ASTM D2866-94) | 0,5 % |
|  | Dureza (ASTM D3802-79) | > 97 % |
|  | Mistura quando embalado (ASTM D2867-91) | < 3 % |
|  | Área Superficial (Método B.E.T.) | 1050 m2/g |
|  | Nº Iodo (JIS K1470-67) | 1000 mg/g |
|  | Azul de Metileno (Espectrofotómetro) | 20 g/100 g |
|  | *** Gama de carvão ativado granular destinado á adsorção de cloro e de contaminantes orgânicos dissolvidos na água.. *** Fabricado a partir de qualidade selecionada de carbono mineral e vegetal natural, por processo de ativação térmica rigorosamente controlada, destinada á obtenção de uma elevada área estrutural residual permitindo a retenção de substancias orgânicas de baixo e elevado peso molecular. *** Carvão Ativado de alta densidade e boa resistência á abrasão e á pressão mecanica. *** PURASORB 630GR Carvão Ativado requere uma lavagem periódica em contra corrente, para eliminar os resíduos acumulados, antes de regressar ao filtro. |  |